# Direction for use

FlowCor Duo

composite dual-cure flowable material for the restoration of tooth core

PURPOSE

Flowable dual-cure composite material "FlowCor DUO" is used in therapeutic and orthopedic dentistry for the buildup of tooth core and the fixation of pins.

PROPERTIES.

"FlowCor DUO" composite material has high plasticity and thixotropy, is easy to mix, has high strength, radiopacity. It can easily fill cavities and undercuts.

The composite material consists of two pastes: catalytic and universal, - which are contained in dual-chamber syringe. They are mixed at the ratio of 1:1, either in the special mixer or by hand.  Light-cured with the wavelength of 450 - 500 nm with a device having the light density of 600 mw/cm2. Working time is 3 minutes. If not exposed to light "FlowCor DUO" composite material is self-cured for 8 minutes maximum.

The set includes dual-cure adhesive “FlowCor Duo” which consists of basic liquid and catalyst liquid (activator of self-cure process). Time of light cure is 20 seconds with light of 450 - 500 nm. Time of self-cure of the adhesive – not more than 10 minutes.

CLINICAL PROCEDURE

Buildup of tooth core: After preparing the cavity, it should be rinsed, dried and then etched with the etching gel for not more than 20 seconds. Then wash it for 20 seconds, dry and fix a matrix. Then prepare the dual-cure adhesive: mix 1:1 main adhesive liquid “FlowCor DUO” and catalytic liquid (activator) “FlowCor DUO”. Time of mixing: 10 seconds. Place the adhesive mixture into cavity with the use of applicator and rub not less than 15 seconds, then dry with air not less than 10 seconds and cure with light of 450 - 500 nm during 20 seconds. The treated surface should be shiny, if it is not - the procedure of adhesive treatment should be repeated.

Insert “FlowCor DUO” composite material in the cavity with the use of disposable needle mixer. Aim the needle into the cavity and slightly push the piston, filling the cavity from bottom to the top, avoiding air getting into the filling. Cure every section of the construction with light for 30 seconds. Correction of the tooth core with restorative/rotary instruments may be started 10 minutes after curing.

If composite material is mixed by hand: place both pastes, catalytic and universal on the mixing pad, by gently pressing the stock of the syringe. Mix with a polymer spatula for 20 seconds, and start modeling the tooth core. The time of modeling should not exceed 3 minutes.

Fixation of pins by “FlowCor DUO” composite material: after endodontic treatment the root channel should be prepared for pin installation, etched with etching gel for not less than 20 seconds, rinsed with water for not less than 20 seconds, dried without overdrying and then place and cure the adhesive system “FlowCor DUO” (see above).

Then insert the mixed “FlowCor DUO” composite material in the cavity with the use of channel filler and accurately place therein the prepared pin, holding it firm to avoid displacement of the pin, cure with light for not less than 30 seconds. After that start modeling the tooth core, curing every section of the construction with light for 30 seconds. Correction of the tooth core with restorative/rotary instruments may be started 10 minutes after curing.

CONTRAINDICATION

Permit no contact with eugenol-containing materials.

STORAGE

"FlowCor DUO" material should be stored in a dry place, protected from direct sunlight. It preserves validity according to the following temperature range:

- + (5 ÷ 12) ° C - 2 years;

- + (12 ÷ 24) ° C - 1 year.